## Slide 1
EFFECT OF BORON CROSSLINKER AND VARIOUS BREAKERS ON THE FORMATION OF GUAR GUM FRACTURING FLUID RESIDUE
Dewi Asmorowati1, Dedi Kristanto1, Mia Ferian Helmy1, Susanti Rina1, Sukma Bayu Yusanto2, Wahyu Endranaka2
{dewi.asmorowati@upnyk.ac.id,
1 Petroleum Engineering Department, UPN Veteran Yogyakarta
2 PT. Bukit Apit Bumi Persada
Correspondence author: dewi.asmorowati@upnyk.ac.id

## Slide 2
Introduction
Result and Discussion
Conclusion
Agenda

## Slide 3: INTRODUCTION
1

## Slide 4
Some additive can cause any residue after it’s added to base fracturing fluid and can plug the pore throat and decreasing permeability in invaded zone. This research was conducted using compatibility test between Guar Gum based fracturing fluid and boron as crosslinker and three type of breaker. The types of breaker used include oxidizer, acid, and encapsulated breaker.
INTRODUCTION

## Slide 5: Result and Discussion
2
LABORATORIUM PERAGAAN DAN SIMULASI PEMBORAN
JURUSAN TEKNIK PERMINYAKAN UPNVY

## Slide 6
This research is done in PT. Bukitapit Bumi Persana laboratory. The test procedures of residue concentration are:
Weight sample based on formulation
Mixing additive in mixing blender until done
Check viscosity of base gel based on specification
Added base gel with buffer, crosslink and breaker with on-fly condition in mixing blender
Put gel fracturing into water bath until break, see figure 1.
After break, filter the precipitate with HTHP Filter Press
Weight of the wet residue (Figure 2), dried in oven with temperature 105 0C
Weight of the dried residue in analytical balance
RESULT AND DISCUSSION
% Residue =

## Slide 7
RESULT AND DISCUSSION
Boron Crosslinker | Oxidizer Breaker | Weight of Sample (g) |  | % Dry Residue
 |  | Wet Residue | Dry Residue | 
0.2% | 0.40% | 12.65 | 0.59 | 12.29 %
0.4% | 0.40% | 14.68 | 1.52 | 31.67 %
0.6% | 0.40% | 15.29 | 2.69 | 56.04 %
Average |  |  |  | 33.33 %
Table 1. Experiment Results with Oxidizer Breaker
Boron Crosslinker | Oxidizer Breaker | Weight of Sample (g) |  | % Dry Residue
 |  | Wet Residue | Dry Residue | 
0.2% | 0.80% | 9.34 | 1.26 | 26.25 %
0.4% | 0.80% | 14.94 | 2.59 | 53.96 %
0.6% | 0.80% | 14.60 | 2.65 | 55.21 %
Average |  |  |  | 45.14 %
Boron Crosslinker | Oxidizer Breaker | Weight of Sample (g) |  | % Dry Residue
 |  | Wet Residue | Dry Residue | 
0.2% | 0.20% | 15.10 | 1.68 | 35.00 %
0.4% | 0.20% | 14.03 | 1.67 | 34.79 %
0.6% | 0.20% | 13.42 | 1.40 | 29.17 %
Average |  |  |  | 32.99 %
Table 2. Experiment Results with Acid Breaker
Table 3. Experiment Results with Encapsulated Breaker

## Slide 8
RESULT AND DISCUSSION
Fig. 1. Aged fracturing fluid in water bath until break
Fig. 2. Wet Residue of 40 system Guar Gum with 0.2% crosslinker and 0.4% oxidizer breaker

## Slide 9: CONCLUSION
3
LABORATORIUM PERAGAAN DAN SIMULASI PEMBORAN
JURUSAN TEKNIK PERMINYAKAN UPNVY

## Slide 10
The experiment shows 40 systems Guar Gum fracturing fluid is compatible with 0.2% crosslink boron and 0.4% oxidizer breaker.
The increase in crosslink concentration indicates the amount of polymer content in the fracturing fluid is directly proportional to the amount of residue produced.
Encapsulated breaker has stable performance due to increasing concentration of boron crosslinker.
CONCLUSION

## Slide 11
LABORATORIUM PERAGAAN DAN SIMULASI PEMBORAN
JURUSAN TEKNIK PERMINYAKAN UPNVY
THANK YOU